Thermafiber® SAFB™

Section 09 81 16
December 15, 2017
ACOUSTIC BLANKET INSULATION

Page 7

Thermafiber® SAFB™ insulation is intended for use as a sound absorptive material within various load bearing and non-load bearing sound and fire rated wall and ceiling construction assemblies.
Thermafiber® SAFB™ insulation provides enhanced acoustical performance and is non-combustible, moisture resistant, non-corrosive and vermin resistant. 

Thermafiber® SAFB™ insulation supports sustainable design strategies for projects seeking compliance with LEED, Green Globes and other sustainable performance targets. Thermafiber® SAFB™ insulation contains a minimum 70% recycled content, has been issued a Bronze Material Health Certificate from Cradle to Cradle and has obtained an Environmental Product Declaration (EPD) certified by UL Environment.
Thermafiber® SAFB™ insulation is not recommended for thermal resistant rated construction assemblies. Use Thermafiber® UltraBatt™ where thermal resistant rated mineral wool batt insulation is required. 

Part 1 General
1.1 SECTION INCLUDES
In this article, select the components or assemblies that are intended to be part of the content of this section and will not be included in other sections.
.1 Sound absorptive batt insulation in [fire rated][and][sound rated][wall][floor][and][ceiling] construction.
1.2 RELATED SECTIONS
In this article, indicate those sections that inter-rely on this section.  The listing below is only partial and should be edited to include those sections specific to the project that describes subjects or products that affect this section directly.
.1 Section [06 11 00 - Wood Framing]:  Sound absorptive insulation.

.2 Section [09 21 16 - Gypsum Board Assemblies]:  Sound absorptive insulation.
.3 Section [09 51 13 - Acoustic Panel Ceilings].
1.3 REFERENCES
Edit this article after editing the rest of this section. Only list reference standards below, that are included within the text of this section, when edited for a project specification - delete other references that do not apply.
Both Canadian and US standards are listed and in some cases the test methods and acceptance criteria are the same. It is suggested that Canadian standards be referenced whenever possible, while the US standards are included to evaluate cited test results from competing manufacturers
.1 ASTM C423-17 - Standard Test Method for Sound Absorption and Sound Absorption Coefficients by the Reverberation Room Method.

.2 ASTM C665-12 - Standard Specification for Mineral-Fiber Blanket Thermal Insulation for Light Frame Construction and Manufactured Housing.
.3 ASTM C795-08(2013) - Standard Specification for Thermal Insulation for Use in Contact with Austenitic Stainless Steel.

.4 ASTM C1104/C1104M-13a - Standard Test Method for Determining the Water Vapor Sorption of Unfaced Mineral Fiber Insulation.

.5 ASTM C1338-14 - Standard Test Method for Determining Fungi Resistance of Insulation Materials and Facings.

.6 ASTM E84-16 - Standard Test Method for Surface Burning Characteristics of Building Materials.

.7 ASTM E136-16a - Standard Test Method for Behavior of Materials in a Vertical Tube Furnace at 750°C.

.8 CAN/ULC-S102-10 - Standard Method of Test for Surface Burning Characteristics of Building Materials and Assemblies.
.9 CAN/ULC-S114-05 - Standard Method of Test for Determination of Non-Combustibility in Building Materials.

.10 CAN/ULC-S129-15 - Standard Method of Test for Smoulder Resistance of Insulation (Basket Method).

.11 CAN/ULC-S702-14 - Standard for Mineral Fibre Thermal Insulation for Buildings.
.12 ISO 14025:2006 - Environmental labels and declarations - Type III environmental declarations - Principles and procedures.
1.4 SYSTEM DESCRIPTION
Edit and use this article carefully; restrict statements to describe the combined result of the components used to piece together an operating or functional assembly.  Do not repeat statements from the SECTION INCLUDES article.
.1 Assembly of components includes materials providing:
.1 Continuity of acoustically-rated assemblies [in conjunction with sealant materials in Section [____]].
.2 Non-combustibility of fire resistant wall, floor and ceiling assemblies.

1.5 ADMINISTRATIVE REQUIREMENTS
.1 Section 01 31 00:  Project management and coordination procedures.
.2 Coordination:
.1 Coordinate with other work having a direct bearing on work of this section.
.2 Coordinate the work with Section [______] for installation of acoustic seal materials.
.3 Coordinate placement of loose-laid acoustic blanket insulation with weight limitations of suspended ceiling assemblies at Section [09 51 13].
1.6 SUBMITTALS FOR REVIEW
Do not request submittals if this specification section or drawings sufficiently describe the products of this section - or if proprietary specifying is used.  This requested review of submittals increases the possibility of unintended variations to the contract documents, thus increasing a consultant's liability.  The following submittals are intended for review to determine eligibility for the project.
.1 Section 01 33 00:  Submission procedures.
.2 Product Data:  Provide data on product characteristics, performance criteria and limitations.
.3 Manufacturer's Certificate:  Certify that Products meet or exceed specified [requirements][
sustainability standards certifications].

1.7 SUBMITTALS FOR INFORMATION
The following submittals are for information only; do not request these submittals if the information submitted will be assessed for acceptability.
.1 Section 01 33 00:  Submission procedures.
When manufacturer's instructions for specific installation requirements are referenced in Part 3 - Execution, include the following request for submittal of those instructions.  Edit the Part 3 statements to avoid conflict with manufacturer's instructions.

.2 Installation Data:  Manufacturer's special installation requirements, including special procedures, perimeter conditions requiring special attention [and [____]].

Include the following ONLY if specifying for a LEED project.  Specify only the technical requirements necessary to achieve the credits desired for this project.
.3 Sustainable Design:
.1 Section [01 35 18]:  LEED documentation procedures.
.2 Provide required LEED documentation for Product [recycled content] [regional materials] [low-emitting materials].
1.8 CLOSEOUT SUBMITTALS
The following submittals are for project close-out purposes; do not request these submittals if the information submitted will be assessed for acceptability.
.1 Section [01 78 10]:  Submission procedures.
Include the following ONLY if specifying for a LEED project.
.2 Sustainable Design Closeout Documentation:  [_____].
1.9 QUALITY ASSURANCE

.1 Sustainability Standards Certifications:

.1 Insulation products shall comply with the requirements of the Cradle to Cradle Certified Product Standard, evidenced by a Bronze Material Health Certificate.
.2 The manufacturer shall disclose insulation product's environmental impacts determined in accordance with ISO 14025, evidenced by an Environmental Product Declaration.
1.10 DELIVERY, STORAGE, AND PROTECTION

.1 Section 01 61 00:  Transport, handle, store, and protect products.

.2 Deliver products in their original packages.
.3 Store products in weather protected environment, clear of ground and moisture and protected from direct exposure to sunlight.

Part 2 Products
2.1 MANUFACTURERS
.1 Manufacturer - Basis of Design: 

.1 Thermafiber Inc.

1 Owens Corning Parkway

Toledo, OH, 43659

Toll Free: 1-800-GET-PINK
Website: www.thermfiber.ca
.2 English-language Contact: Matthew Schiedel

E-mail: matthew.schiedel@owenscorning.com
Telephone: 1-844-304-1623

.3 French-language Contact: Salvatore Ciarlo
E-mail: Salvatore.ciarlo@owenscorning.com
Telephone: 1-800-504-8294

.2 Substitutions:  [Not permitted] [Refer to Section 01 62 00].
2.2 PERFORMANCE CRITERIA

.1 Noise Reduction Coefficient (NRC): [0.95 at <50 mm><<2 inch>>][1.05 at <75 mm><<3 inch>>][1.20 at <102 mm><<4 inch>>][1.20 at <152 mm><<6 inch>>] thickness.
.2 Fire Resistance: Certified by ULC/UL for use in fire-resistant rated assemblies.

Surface burning characteristics for CAN/ULC-S702 Type 1 products to have flame-spread classification not exceeding 25 and smoke-developed classification not exceeding 50 tested according to CAN/ULC-S102. Values noted below are actual results, well below required limits.

.3 Surface Burning Characteristics: [CAN/ULC-S102][ASTM E84].
.1 Flame Spread: 0.

.2 Smoke Developed: 0.

.4 Non-combustible when tested in accordance with [CAN/ULC-S114][ASTM E136].

Smoulder resistance for CAN/ULC-S702 Type 1 product requires the insulation to have a mean mass loss less than or equal to 2% tested according to CAN/ULC-S129. Value noted below is actual result, well below required limits.

.5 Smoulder resistance: 0.02% to CAN/ULC S129.

.6 Moisture Absorption to ASTM C1104: < 0.03% by volume.

.7 Fungi resistant when tested in accordance with ASTM C1338.
.8 Non-corrosive when tested in accordance with ASTM C665 (steel, aluminum and copper) and ASTM C795 (stainless steel).
.9 Recycled Content: Minimum 70%.

2.3 MATERIALS
Edit these paragraphs to suit the project’s wall assemblies, specifically wood or steel framing.  Delete items not required.

.1 Mineral Wool Acoustic Batt Insulation:  [CAN/ULC-S702] [ASTM C665] Type 1; preformed mineral fibre, friction fit, conforming to the following:
.1 Wood-framed applications:
.1 Thickness: [<25 mm><<1 inch>>][<38 mm><<1.5 inch>>][<50 mm><<2 inch>>][<64 mm><<2.5 inch>>][<75 mm><<3 inch>>][<89 mm><<3.5 inch>>][<102 mm><<4 inch>>][<125 mm><<5 inch>>] [<152 mm><<6 inch>>][<180 mm><<7 inch>>][<203 mm><<8 inch>>].
.2 Size:  [<381 mm><<15 inch>>][<584 mm><<23 inch>>] width x <1194 mm><<47 inch>> length.
.2 Steel-framed applications:

.1 Thickness: [<25 mm><<1 inch>>][<38 mm><<1.5 inch>>][<50 mm><<2 inch>>][<64 mm><<2.5 inch>>][<75 mm><<3 inch>>][<89 mm><<3.5 inch>>][<102 mm><<4 inch>>][<125 mm><<5 inch>>] [<152 mm><<6 inch>>][<180 mm><<7 inch>>][<203 mm><<8 inch>>].

.2 Size:  [<406 mm><<16 inch>>][<610 mm><<24 inch>>] width x <1219 mm><<48 inch>> length.

.3 Facing:  Unfaced.
.4 Acceptable Product: Thermafiber® SAFB™.

Insulation accessories are project specific; edit the following to suit. Delete items not required.

2.4 ACCESSORIES

.1 Wire Mesh:  Galvanized steel, hexagonal wire mesh.
.2 Wood Strapping: Refer to Section [06 10 00].

Part 3 Execution
3.1 EXAMINATION
.1 Section 01 70 00:  Verify existing conditions before starting work.
.2 Examine installation conditions and ensure:

.1 Substrate, adjacent materials, and insulation are dry and ready to receive insulation.
.2 Acoustic sealants required at [steel][wood][stud framing][concrete masonry unit wall] junctions with adjacent building components or at mechanical, electrical and other services are installed.

.3 Ensure structural and firestop elements, mechanical and electrical services to be covered by the insulation have been inspected.

.4 Do not commence installation until base work has been corrected and inspections completed.
3.2 INSTALLATION
.1 Place acoustics blankets where indicated on drawings to [thickness indicated on drawings][thickness indicated in acoustic assembly test report].

.2 Partitions, floors and ceilings constructed of [steel studs][wood studs][furred concrete or concrete masonry]:

.1 Install blankets friction-fit between [framing][furring] of [wall][floor][and] [ceiling] spaces with tight fitting joints free of sags, folds, voids or open joints.  Do not compress insulation.
Select one or more of the appropriate option statements in the following paragraph. Delete if not required.
.2 [Retain insulation in place with wire mesh secured to framing members] [Retain insulation in place with wood strapping secured to framing members] [Retain insulation in place with resilient metal channel secured to framing members].  

.3 Acoustic panel ceiling assembly:

.1 Lay acoustic blankets over acoustic panel ceiling assembly free of sags, folds, voids or open joints.

.2 Overlap joints in multiple layer installations.

.4 Cut and fit insulation tightly around mechanical and electrical services within the plane of insulation filling all voids. Cut insulation with a serrated knife for custom fitting. Do not compress insulation.
Ensure clearances meet local building safety regulations and code requirements. For electrical fixtures housed in a CSA-approved insulated enclosure, prescribed clearances are not required unless indicated otherwise by the fixture’s manufacturer.

.5 Keep insulation minimum 75 mm from heat-emitting devices, such as recessed fixtures (which are not IC rated), and minimum 50 mm from sidewalls of CAN/ULC-S604 chimneys and CSA-B149.1 and CSA-B149.2 type B and L vents.

Include the following paragraph as required.
.6 Coordinate work of this section with construction of acoustic panel ceiling assemblies specified in Section [09 51 13].
Include the following paragraph as required.

.7 Coordinate work of this section with construction of gypsum board specified in Section [09 21 16].
3.3 SCHEDULES
The following article will assist in preparing a schedule for the project.   The following schedules included are EXAMPLES only.  Edit the paragraphs below to create a schedule for the components specified in this section.  Do not repeat statements that may exist on drawings.
.1 Meeting Room Ceilings:  [<75 mm><<3 inch>>] thickness, loose-laid over ceiling panels.
.2 Meeting Room Walls:  [<64 mm><<2.5 inch>>] thickness [as required to fill depth of framing].

END OF SECTION
